Mission Peak Optics Inc.

Portable Thin Film Measurement System MP100-S

Easy to use + Low Cost + Compact Size + Flexibility = High Performance

Specifications (MP100-S):

Scanning range:			380 nm to 950 nm Standard

Optional range:			200 nm to 2500 nm

Spectrum resolution:		2 nm in Visible, 4 nm in NIR

Precision:				0.2 nm

Measuring speed:			2 seconds (Standard Wavelength Range)

Measurement specification:

|  | 1st Layer | 2nd Layer | 3rd Layer 1σ 0 - 10,000 Å 5 Å | 4 th Layer |
| --- | --- | --- | --- | --- |
| Film Type | Objective | Range | 1σ | Range | 1σ | Range | 1σ | Range | 1σ |
| P1/P2/ITO/SiO2/Glass | Probe | 100 - 3,000 Å | 3Å | 100-3000 Å | 3Å | 100-1500 Å | 3Å | 100-1500 Å | 3Å |
| Oxide/Si | Probe | 200 ,- 30,000 Å | 2Å |  |  |  |  |  |  |
|  |  | 30,000 ,- 050,000 Å | 5Å |  |  |  |  |  |  |
|  |  | 50,000 - 100,000 Å | 20Å |  |  |  |  |  |  |
| Nitride/Si | Probe | 150 ,- 020,000 Å | 2Å |  |  |  |  |  |  |
| Photoresist/Si | Probe | 500 ,- 020,000 Å | 5Å |  |  |  |  |  |  |
| Nitride/Oxide/Si | Probe | 150 ,- 020,000 Å | 5Å | 150-20,000Å | 5Å |  |  |  |  |
| Poly/Oxide/Si | Probe | 100 ,- 5,000 Å | 5Å | 0-10,000Å | 5Å |  |  |  |  |
| Oxide/Poly/Oxide/Si | Probe | 100 ,- 010,000 Å | 5Å | 0-10,000Å | 5Å | 100-10,000 Å | 5Å |  |  |
| Oxide/Al | Probe | 2,000 ,- 020,000 Å | 5Å |  |  |  |  |  |  |
| Photoresist/Cr | Probe | 500 ,- 020,000 Å | 5Å |  |  |  |  |  |  |
| Oxide/NiFe | Probe | 2,000 ,- 020,000 Å | 5Å |  |  |  |  |  |  |
| Photoresist/Glass | Probe | 500 ,- 20,000 Å | 5Å |  |  |  |  |  |  |
| ITO/Oxide/Glass | Probe | 100 - 3,000 Å | 2Å | 100-2,000Å | 2Å |  |  |  |  |
| Very Thick film | Probe | 1000 - 500,000 Å | 100Å |  |  |  |  |  |  |
| Customized film types are available for your applications. |  |  |  |  |  |  |  |  |  |

Measuring spot size: 3 to 5 mm diameter

Mission Peak Optics Inc.

46941 Rancho Higuera Road, Fremont, CA 94539 USA

Tel: (510) 438-0384		Fax: (510) 438-9795

Website: www.missionpeakoptics.com 	Email: sales@missionpeakoptics.com

# Text boxes

Spectrometer

The MP100-S system comes standard with a portable spectrometer, optical probe mounted on a manual X,Y stage, and a laptop computer pre-loaded with MPO software. At the price of around $12,000, it cannot be beat.  The software contains hundreds of pre-loaded film recipes with the ability to create and edit new ones.  The MP100-S can measure Oxide, Nitride, Photoresist, Polysislicon, CIE chromaticity, cell gap, color filter thickness, as well as polyimide/ITO. The portability of this compact system allows you to put the probe into the Measurement site.

USB

The MP100-S probe can be dismounted from the stage and held by hand to access hard to reach areas.   Applications include reflectivity of a surface, textile color of a material, liquid concentration and material inspection all with real-time spectral analysis.  The probe can be configured for a working distance up to 6 inches with a varying measurement spot size.

The MP100-S positioning mechanism is set by a X, Y stage. Allowing you to quickly locate the sample position. When the selected sampling position has been reached, measurements can be taken precisely and accurately without the X, Y stage drifting.

There is an add-on option for a programmable X, Y stage from 4 to 12 inches of travel.

MP100-S Portable Thin Film Measurement System

Bifurcated Optical Probe

Light Source

XY stage